## Slide 1: Thermoelectric data teMatDb: ultrahigh quality material transport data
Byungki Ryu,*
J Chung, SJ Park, JH Son, SJ Park, YH Ihm, SD Park
Korea Electrotechnology Research Institute, Korea

## Slide 2: Goal and actions
High-quality data for transport analysis
  Can be used for machine learning
In this work,
  Error analysis
    Error case categorization
    Filter development
    Q-Q analysis
  Distribution and comparison
    Center of mass and boundary for TEPs
    Performance boundaries (singleleg limit)
Open source
  Github repository for data and code
  TE Simulator app using (python, pykeri, streamlit)

## Slide 3: * Ultrahigh quality TE mat. DB for data science and machine learning
QR code for (teMatDb v1.1.1b)
Feature
TE property data
Metadata: composition, process
Error analysis
  Error filter
  Error analysis
Data size
  353 before filtering
  268 high-Q dataset

## Slide 4: Thermoelectric material data digitization
Thermoelectric property
  Property curves on temperature
Sampled, digitized data
  ,
  ,
May contain error
  Digitization error
  Publication error

## Slide 5: Human-labor digitization uncertainty
Data generation, digitization
  (x, y)
  (x’, y’)
Calculate deviation
  (dx=x’-x, dy=y’-y)
Std error is small enough:
  For 3.5 inch wide, Lx=Ly=100
  72-300 dpi figures: less important
    Dpi > 72 would be necessary
    1/ (3inch x 72 dpi) = ~1/200 = 0.5%
  Circle, triangle: less important
  dx/Lx, dy/Ly< ~0.5%
Uncertainty estimation with assumption (df/f is small)
  d(ZT) = (ZT) x sqrt(7) df/f = 3.1 x 3.65 x 0.005 = 0.04
  95% (k=2)  d(ZT)=~0.08 < 0.1
    df/f can be large enough
Normal single-column figure, < 3.5 inch

## Slide 6: Impact of data filter
Starrydata, 20211124
Original filter
  11846
After filter
  (filter1) 9373
  (filter2) 7353
Previous filter (iScience 2021)
  ~30 filters,
  ZT-ZT filter: 70% - 130%
  sampleids_in_fig3a (teps) = 13338
  sampleids_in_fig3b (etas) = 12645
  sampleids_in_df_tep_extended= 11846
teMatDb, v1.1.1b
No filter
  353
After filter
  (filter1) 268
  (filter2) 236
Criteria
  d(avgZT) > 0.1
  d(peakZT) > 0.1
  Max( abs(d(ZT) ) > 0.1
  ZT err := L2(d(ZT))=stdev.s > 0.1
  Max(ZT err)/(peakZT) > 0.2
  Max(ZT err)/(avgZT) > 0.2

## Slide 7: DB stats comparison
Level | Starrydata2 (20211124) |  | teMatDb | 
total | 16420 | 100% | 353 | 100%
physics filter | 13338 | 81% |  | 
TEP-ZT complete set | 11846 | 72% | 353 | 100%
ZT filter, level1 | 9373 | 57% | 268 | 76%
ZT filter, level2 | 7353 | 45% | 236 | 67%
0.1
0.1
0.1
0.1
0.2
0.2
0.1
0.1
0.1
0.1
0.1
0.1
Filter, level1
Filter, level2

## Slide 8: Filtered teMatDb (1.1.1b)

## Slide 9
Before filtering: 353
After filtering: 268
0.1
0.1
0.1
0.1
0.2
0.2

## Slide 10
0.1
0.1
0.1
0.1
0.1
0.1
After filtering: 236
Before filtering: 353

## Slide 11: Filtered Starrydata2 (20211124)

## Slide 12
Original filtering: 11846 sampleids
After filtering: 9373 sampleids
0.1
0.1
0.1
0.1
0.2
0.2

## Slide 13
Original filtering: 11846 sampleids
After filtering: 7353 sampleids
0.1
0.1
0.1
0.1
0.1
0.1

## Slide 14: Data distribution

## Slide 15: Performance and TEP distribution
ZT
Efficiency
Lorenz

## Slide 16: Error case (summary)

## Slide 17: Peak ZT error
1
1
1
1
1: sampleid = 235, ktot != klatt
1
1
1
1

## Slide 18: ZT curve error (TEP smallT)

## Slide 19: ZT curve error (TEP autoTcTh)

## Slide 20: Sample stats (autoTcTh)
teMatDb v1.0
  355 valid samples
ZT error removing (>0.30)
  353 (peak ZT error cases removing)
  345 (ZT curve error cases removing)
ZT error removing (>0.15)
  339 (peak ZT error cases removing)
  314 (ZT curve error cases removing)
314 high-Q samples
Errorsamples
ZT error removing (>0.30)
  [140 156 181 193 235 238 300 415 420]
  +[113 235]
ZT error removing (>0.15)
  [ 1 2 5 26 27 28 79 81 92 95 98 110 113 124 125 129 139 140 151 152 156 165 181 193 210 220 226 235 238 245 254 285 293 300 355 381 409 415 420]
  +[ 1 2 26 79 81 84 95 107 113 129 181 193 235 238 293 415]

## Slide 21: Sample stats (smallT: ZT, TEP range 교집합)
teMatDb v1.0
  355 valid samples
ZT error removing (>0.30)
  353 (ZT curve error cases removing)
  348 (peak ZT error cases removing)
ZT error removing (>0.15)
  339 (ZT curve error cases removing)
  318 (peak ZT error cases removing)
Errorsamples
ZT error removing (>0.30)
  [140 181 235 238 300 415]
  +[113 235]
ZT error removing (>0.15)
  [ 1 2 26 27 28 79 81 92 95 98 110 113 124 125 129 139 140 151 152 165 181 193 210 220 235 238 245 254 285 293 300 355 381 409 415]
  +[ 1 2 26 79 81 84 95 107 113 129 181 193 235 238 293 415]

## Slide 22: Error categorization

## Slide 23: Error analysis
Errors | Incomplete | Insufficient data | Bias error | Extrapolation, ZT mismatch | Resolution error | Extrapolation, but ZT match
D(Peak-ZT) on T TEP |  | 181, 235 | 1, 2, 192, 238, 415 | 113, 193 | 27, 28 | 420
D(Peak-ZT) on T ZT |  | 181, 235 | 1, 2, 192, 238, 415 | 113, 140, 193, 84, 107 | 27, 28 | 5
D(Peak-ZT) on T TEPZT |  | 181, 235, 243 | 1, 2, 192, 238, 415 | 113, 193, 84 | 27, 28 | 
D(peak-ZT) on each T |  | 235 | 1, 2, 192 | 113, 140, 193, 84, 107 |  | 
D(ZT) on TTEP |  | 235 | 1, 2, 192, 238, 415 | 113, 156, 193 | 140, 300 | 
D(ZT) on TZT |  | 235, 243 | 1, 2, 192, 238, 415 | 113, 193, 84, 107 | 140, 300 | 
D(ZT) on TTEPZT |  | 235 | 1, 2, 192, 238, 415 | 113, 193 | 140, 300 | 
TEP missing (k_ph instead of k_tot) |  | 235, |  |  |  | 
Value too high | 243 |  |  |  |  | 
Case categorization |  | 235, 181, 238 | 1, 2, 26, 79, 81, 92, 95, 129, 192, 238, 293, 415 | 84, 107, 113, 181, 193 | 1, 27, 28, 81, 76, 193 | 
Error | Incomplete | Error | Error | Error | Error | Not error
Interpolation test using d(ZT) on TEPZT
Extrapolation test using d(peak-ZT)
Average of D(ZT – ZT): L1, L2, Linf test only for interpolation range
Difference in D(Peak-ZT): peak ZT comparison for each T range

## Slide 24: How to measure error: error measure operators

## Slide 25: Issues
Data gathering
  Well digitized
    Consistent between TEP and ZT  good data
    Inconsistent between TEP and ZT  contaminated, erroneous
  Poorly digitized
    Human error (unit, label): can be fixed
    Resolution issue: in principle, impossible
Data continuation over temperature
  Interpolation
    Piecewise-linear manner
    Barycentric polynomial using Chebyshev node 2nd-kind (see JC’s paper)
  Extrapolation
    constant-extrapolated

## Slide 26: Equations for filter development
Operation definition
Error measure: n+2 measures
  Peak bias filter
  Average bias filter
  Error filter (to see interpolation quality)
Extrapolation risk
  T range uncertainty
1: ZT data and its T range (T1)
2: TEP data and its T range (T2)
ZT and TEP data are all interpolated using piecewise-linear manner.

## Slide 27: Error statistics for hi-Q

## Slide 28: Error measure and table
Measure operations
T range
  delTc, delTh, delT
Bias measure
  Peak bias
  Average bias
Scatter measure
  L1
  L2
  L3, L4
  Linf
Save
T-range record
  [Tc,Th]TEP
  [Tc,Th]ZT
  [Tc,Th]TEPZT
Ten (3+2+5) error record per sample

## Slide 29: Error cleansing

## Slide 30: Error cleansing and classification (left) Error samples (right) cleansed & error classified
ZT error removing (>0.30)
  [140 181 235 238 300 415]
  +[113 235]
ZT error removing (>0.15)
  [ 1 2 26 27 28 79 81 92 95 98 110 113 124 125 129 139 140 151 152 165 181 193 210 220 235 238 245 254 285 293 300 355 381 409 415]
  +[ 1 2 26 79 81 84 95 107 113 129 181 193 235 238 293 415]
Digitization error, Cleansed: Axis error
  1 (sigma y axis digitization error corrected),
  28, 253, 355 (poor resolution 재추출 후, error reduced)
notError
  5, 156, 420 (T range mismatch, but data is ok)
Lack of data, cannot reproduce
  235 (k_el in k_tot, deleted)
ZT error (biased, publication error)
  26, 95, 125, 415 (checked, over ZT)
  81 (checked, under ZT)
Extrapolation
  84, 107, 113 (TEP fitted and ZT made?)
Interpolation cannot reproduce
  27, 300, 409 (sigma phase transition, resolution, cannot interpolate)
teMatDb excel file 과 redigitizing (문헌다시비교)
에러로그 기록(작성중)  error_cleansing_log.xlsx

## Slide 31: Cleansed, corrected, notError

## Slide 32: Sampleid = 1
Literature
  10.1038/NCHEM.955
  Biswas, Kanatzidis, Nature Chem
ZT over reported
  ZT author declared: 1.7
  ZT reevalulated from TEP: 1.5
Possible error origin
  Poor resolution
ZT over declared
Corrected, now no error

## Slide 33: Sampleid=1 (재추출) digitization error: sigma y2 axis corrected
before
after
https://tematdb-v1-0-0-main-v1-0-2-abc.streamlit.app/
v1.1

## Slide 34: Sampleid = 2
Literature
  10.1038/nature11439
  Biswas, Kanatzidis, Nature
ZT over reported
  ZT author declared: 2.2
  ZT reevalulated from TEP: 1.5
Possible error origin
  Extrapolation
ZT under declared
Corrected, now no error

## Slide 35: Sampleid=28 (재추출) poor resolution, but overcome
before
after
https://tematdb-v1-0-0-main-v1-0-2-abc.streamlit.app/
v1.1

## Slide 36: Sampleid = 253 // teMatDb error, updated
Keri error, wrong sample
updated

## Slide 37: Sampleid=355 (재추출) poor resolution, but overcome
before
after
https://tematdb-v1-0-0-main-v1-0-2-abc.streamlit.app/
v1.1

## Slide 38: T range mismatch, not error

## Slide 39: Sampleid=5, 156, ZT range small, avg ZT mismatch, but not error
Avg ZT on T of TEP != avg ZT on T of ZT.
T of TEP != T of ZT

## Slide 40: Sampleid = 420 (not error)
T range difference
  ZT T range smaller than TEP T range
  As ZT is extrapolated to TEP T range, it is inconsistent to TEP ZT.

## Slide 41: Extrapolation, high ZT error

## Slide 42: Sampleid=84 (extrapolation)
No high-T seebeck

## Slide 43: Sampleid = 113, TEPs are extrapolated
ZT can not be reproduced from measured TEPs

## Slide 44: Sampleid = 113, TEPs are extrapolated
Largely extrapolated value
ZT author declared: 1.47
ZT reevaluated from tep: 1.15

## Slide 45: Biased (can not reproduce, even after redigitizing)

## Slide 46: Sampleid=95 (publication error)

## Slide 47: Sampleid = 415
Literature
  10.1002/aenm.201601450
  LD Zhoa, Adv E Mater
ZT over reported
  ZT author declared: 2.3
  ZT reevalulated from TEP: <2.0
Possible error origin
  Error from mismatch between PF and conduction

## Slide 48: Lack of data

## Slide 49: Sampleid = 235, K_elec is missing
Difficult to get a dataset
No k_tot figure, though k_elec equation is given
k_elec = L sigma T (Lorenz-Wiederman Law, L = 2x10^-8)
k_latt = k_tot – k_ele
Inconsistent notation for compositions

## Slide 50: APPENDIX.1. Error cases

## Slide 51: Sampleid = 140, computation
T range of TEP is smaller than T range of ZT
Mismatch from extrapolation

## Slide 52: Sampleid = 156
T range of TEP is smaller than T range of ZT
Mismatch from extrapolation

## Slide 53: Sampleid = 181 // exponential or extrapolation or publication error

## Slide 54: Sampleid = 192, 193 (doi=10.2320/matertrans1989.33.851)

## Slide 55: Sampleid = 238
Check several times
Check exchange persons
But problem remained
Might be publication error

## Slide 56: Sampleid = 300
Rapidly varying TEP curves, difficult to interpolate
Reevalutation overestimate ZT owing to poor interpolation by us